README file

Dataset Title: Dataset of Toward Sustainable Gel Chemistry: Supramolecular Gelation of Amino Acid Derivatives in Green Solvents

Dataset Authors: Demetra Giuria, Elisa Cicalinia, Devis Montronia, Claudia Tomasini

Affiliations: a. Department of Chemistry “Giacomo Ciamician”, University of Bologna, via Gobetti, 85, 40129 Bologna, Italy

Dataset contact person: Demetra Giuri, Department of Chemistry “Giacomo Ciamician”, University of Bologna, Via P. Gobetti 85, 40129 Bologna, Italy, demetra.giuri2@unibo.it

Dataset License: this data set is distributed under a Creative Commons Attribution 4.0 International (CC BY 4.) license, https://creativecommons.org/licenses/by/4.0/.

Publication year: 2026

DATASET CONTENTS

The dataset consists of a folder named DATASET that contains:

- A Readme file in .doc format

The following subfolders:

- “Amplitude Sweep”

- “Amplitude Sweep_Pre and Post Temperature”

- “Frequency Sweep”

- “FT-IR”

- “NMR”

- “Temperature Sweep”

- “Thixotropy”

The acronyms used for the analyses are:

Amplitude Sweep (AS)

Frequency Sweep (FS)

Thixotropy (Thix)	

For each test, the acronym is followed by the name of the compound analysed. 	
According to the corresponding nomenclature in the paper (D. Giuri, E. Cicalini, D. Montroni, C. Tomasini,  Toward Sustainable Gel Chemistry: Supramolecular Gelation of Amino Acid Derivatives in Green Solvents, Ind. Eng. Chem. Res. 2026; https://doi.org/10.1021/acs.iecr.6c00523) the molecules are named A, B, C, D, E and F; the gels are named with the letter corresponding to the molecule and numbers corresponding to the green solvent used to prepare them (1, 2, 3, 4, 5, 6, 7, 8), always in accordance with the paper.

Dataset documentation

Abstract

The dataset contains the NMR data as .fid files and the FT-IR as Origin files, used to characterize derivatives of L-Dopa and L-Tyr that behave as low molecular weight gelators. The ability of these gelators to form gels in different green organic solvents was evaluated through a deep rheological characterization, which is also reported in the dataset as Origin files.

Content of the files

The attached dataset includes the characterization of gelators molecules (NMR and IR) and of the corresponding supramolecular gels, deriving from a gel screening in green organic solvents. The dataset corresponds to Figures 3, 4, 5 and 7 of the main paper and Figures S2 to S8 of the Supporting Information of the publication: D. Giuri, E. Cicalini, D. Montroni, C. Tomasini,  Toward Sustainable Gel Chemistry: Supramolecular Gelation of Amino Acid Derivatives in Green Solvents, Ind. Eng. Chem. Res. 2026. https://doi.org/10.1021/acs.iecr.6c00523

In particular:

- 1 folder named NMR containing 4 subfolders named after compounds B, C, E and F, each containing the original fid of 1H, 13C and gCOSY spectra for the corresponding compounds.	 
The software used for acquisition was OpenVnmrJ. The files can be opened via the abovementioned softwares or via MestreNova or SpinWorks, or any other software for NMR data elaboration.

- 1 folder named FT-IR containing 4 files, corresponding to the FT-IR of compounds B, C, E and F. The files OPJ were created with Origin8.5 and can be opened with compatible Origin versions or OriginViewer.

- 1 folder named Amplitude Sweep that contains the Origin files corresponding to the amplitude sweep analyses of the gels. The files OPJ were created with Origin8.5 and can be opened with compatible Origin versions or OriginViewer.

- 1 folder named Amplitude Sweep_Pre and Post Temperature contains the Origin files corresponding to the Amplitude Sweep test, before and after Temperature annealing. The files OPJ were created with Origin8.5 and can be opened with compatible Origin versions or OriginViewer.

- 1 folder named Frequency Sweep contains the Origin files corresponding to the Frequency sweep analyses of the gels. The files OPJ were created with Origin8.5 and can be opened with compatible Origin versions or OriginViewer.

- 1 folder named Temperature Sweep contains the Origin files corresponding to the temperature sweep analyses of the gels. The files OPJ were created with Origin8.5 and can be opened with compatible Origin versions or OriginViewer.

- 1 folder named Thixotropy contains the Origin files corresponding to the step-strain analyses of the gels. The files OPJ were created with Origin8.5 and can be opened with compatible Origin versions or OriginViewer.

Methodologies

- NMR spectra were recorded with a Varian (Palo Alto, CA, USA) Inova 400 spectrometer at 400 MHz (1H NMR) and at 100 MHz (13C NMR). Chemical shifts are reported in δ values relative to the solvent peak.

- High quality infrared spectra (64 scans) were obtained at 2 cm−1 resolution with an ATR-IR Agilent (Santa Clara, CA, USA) Cary 630 FTIR spectrometer. A Jasco (Mary’s Court, MD, USA) P-2000 Polarimeter was used to check the optical rotatory power of the compounds.

- The rheological analyses were performed using an Anton Paar (Graz, Austria) MCR 102 rheometer. A cup and vane measuring system was used, setting a gap of 2.2 mm. The gel samples (2.5 mL) were prepared in glass test tubes that fit in the rheometer and were left to rest for 16 h at room temperature before the analysis.

- Oscillatory amplitude sweep experiments were performed at 23 °C using a Peltier control system and the data points were collected (γ: 0.01 – 100%) using a constant angular frequency of 10 Hz.	
- Frequency sweep experiments were performed at 23 °C, in a frequency range ω=0.1 – 100 rad/s, using a constant shear strain γ=0.01%. 	
- Thixotropy experiments (step strain) were performed on the gels, subjecting the sample to consecutive rest, deformation and recovery steps, at a fixed frequency of ω = 10 rad s−1. The rest step was performed by keeping the sample at a constant strain γ = 0.03%, i.e., within the LVE region (20 points, 15 s each). The deformation step was performed by applying a constant strain of γ = 300%, i.e., above the LVE region of the sample (20 points, 15 s each) to break the gel network. The recovery step was performed by keeping the sample at a constant strain γ = 0.03%, i.e., within the LVE region for a longer time (50 points, 15 s each). The deformation and recovery cycles were repeated two times.	
- Temperature sweep tests were performed at a constant γ = 0.046% and ω = 10 rad s−1. The temperature ramp was built in the following way:	
1. heating from 23 °C to 75 or 93 °C depending on the Tgel of the sample previously observed in vial 
2. constant temperature for 5 to 10 minutes	
3. cooling ramp arriving to 23 °C	
4. constant temperature (23 °C) for 2 h.

All the rheometer data were collected with the AntonPaar  RheoCompass software  and copied into the Origin files to plot the graphs. When triplicates were performed, the corresponding Origin file reports the three single analyses and/or the Mean±Standard Deviation.

Detailed synthetic procedures for the gelators were reported in the manuscript this dataset refers to (see “References” section).

References
D. Giuri, E. Cicalini, D. Montroni, C. Tomasini, Toward Sustainable Gel Chemistry: Supramolecular Gelation of Amino Acid Derivatives in Green Solvents, Ind. Eng. Chem. Res. 2026. https://doi.org/10.1021/acs.iecr.6c00523