README file

Dataset Title: Dataset of From Fundamental Self-Assembly Studies to Applications in Everyday Life: the Formation of a Supramolecular Shampoo

Dataset Authors: Sofia Chinelli, Demetra Giuri, Claudia Tomasini

Dataset Contributors: Roberta Stile (data collector)

Affiliations: a. Department of Chemistry “Giacomo Ciamician”, University of Bologna, via Gobetti, 85, 40129 Bologna, Italy

Dataset contact person: Demetra Giuri, Department of Chemistry “Giacomo Ciamician”, University of Bologna, Via P. Gobetti 85, 40129 Bologna, Italy, demetra.giuri2@unibo.it

Dataset License: this data set is distributed under a Creative Commons Attribution 4.0 International (CC BY 4.0) license, https://creativecommons.org/licenses/by/4.0/.

Publication year: 2026

DATASET CONTENTS

The dataset consists of a folder named DATASET that contains:

- A Readme file in .doc format

The following subfolders:

- “AMPLITUDE_SWEEP”

- “FREQUENCY_SWEEP”

- “TEMPERATURE_SWEEP”

- “VISCOSITY”

- “pKa”

The acronyms used for the analyses are:

Amplitude Sweep (AS)

Frequency Sweep (FS)

Viscosity (CSR)	

For each test, the acronym is followed by the name of the compound analysed. 	
According to the corresponding nomenclature in the paper (Sofia Chinelli, Roberta Stile, Demetra Giuri, Claudia Tomasini,  Gels 2026, https://doi.org/10.3390/gels12070589) the gels are named G1, G2, G3, G4, G5, G6, G7 and G8, corresponding to the ingredients used to prepare them, in accordance with the description in the paper.

Dataset documentation

Abstract

The dataset contains the rheological and pKa characterization of 8 formulations (G1 – G8) reported in the dataset as Excel files. The first two formulations are prepared by mixing an anionic surfactant, sodium cocoyl glycinate for G1 and sodium cocoyl alaninate for G2, in water with lactic acid. All the other formula (G3 – G8) are obtained with sodium cocoyl glycinate and the addition of several ingredients to create a supramolecular shampoo. For each formula, the rheological characterization comprises amplitude sweep, frequency sweep and viscosity curves. Only for formulations G1 and G2 also a temperature sweep test was performed, while the stability of the final formula G8 was characterized also after 3 months.

Content of the files

The attached dataset includes the characterization of gel formulations. The dataset corresponds to the rheological analyses of formulations G1 – G8 (see tables below), reported in the paper: From Fundamental Self-Assembly Studies to Applications in Everyday Life: the Formation of a Supramolecular Shampoo, by Sofia Chinelli, Roberta Stile, Demetra Giuri, and Claudia Tomasini, Gels 2026, https://doi.org/10.3390/gels12070589.

Formulations ingredients:

Preparation of G1: SCG (10% w/w) + CAPB (4.5% w/w) + lactic acid

Preparation of G2: SCA (10% w/w) + CAPB (4.5% w/w) + lactic acid

| INGREDIENTS | G3 | G4 |  | G5 | G6 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | (% w/w) | (% w/w) |  | (% w/w) | (% w/w) |  |
| SCG (commercial solution at 22%) | 45.40 | 45.40 |  | 45.40 | 45.40 |  |
| CAPB (commercial solution at 30%) | 15.00 | 15.00 |  | 15.00 | 15.00 |  |
| lactic acid | 2.40 | 2.40 |  | 2.40 | 2.40 |  |
| benzylic alcohol | 0.50 | / |  | / | / |  |
| sodium benzoate | / | 0.19 |  | / | / |  |
| caprylhydroxamic acid/1,2-hexanediol/propanediol | / | / |  | 1.50 | / |  |
| phenoxyethanol and ethylhexylglycerin | / | / |  | / | 0.90 |  |
| deionized water | 36.70 | 37.00 |  | 35.70 | 36.30 |  |
| INGREDIENTS |  |  | G7 |  |  |  |
|  |  |  | (% w/w) |  |  |  |
| SCG (commercial solution at 22%) |  |  | 45.40 |  |  |  |
| CAPB (commercial solution at 30%) |  |  | 15.00 |  |  |  |
| benzylic alcohol |  |  | 0.50 |  |  |  |
| sodium benzoate |  |  | 0.19 |  |  |  |
| lactic acid |  |  | 2.40 |  |  |  |
| deionized water |  |  | 36.51 |  |  |  |

| INGREDIENTS | G8 |
| --- | --- |
|  | % w/w |
| SCG | 45.50 |
| CAPB | 15.00 |
| lactic acid | 2.30 |
| benzyl alcohol | 0.50 |
| sodium benzoate | 0.19 |
| decyl glucoside | 2.50 |
| cetrimonium chloride | 2.00 |
| fragrance | 0.60 |
| water to 100 | 31.41 |
| TOT | 100.00 |

In particular:

- 1 folder named AMPLITUDE SWEEP that contains the Excel files corresponding to the amplitude sweep analyses of the gels G1 – G8.

- 1 folder named FREQUENCY SWEEP contains the Excel files corresponding to the Frequency sweep analyses of the gels G1 – G8.

- 1 folder named Temperature Sweep contains the Excel files corresponding to the temperature sweep analyses of gels G1 and G2.

- 1 folder named VISCOSITY contains the Excel files corresponding to the viscosity curves of gels G1 – G8.

- 1 folder named pKa contains the Excel files corresponding to the titration of a 10% solution of SCG (sodium cocoyl glycinate) and SCA (sodium cocoyl alaninate) with HCl. The measurements are performed in triplicate (1, 2 and 3), with the calculation of mean and standard deviation.

The dataset folder is organized as follows:

20260626_SupramolecularShampooGel/

├── 20260626_SupramolecularShampooGel_Readme.docx

├── AMPLITUDE_SWEEP

│   ├── AS_G1.csv

│   ├── AS_G2.csv

│   ├── AS_G3.csv

│   ├── AS_G4.csv

│   ├── AS_G5.csv

│   ├── AS_G6.csv

│   ├── AS_G7.csv

│   ├── AS_G8_3months_45C.csv

│   ├── AS_G8_3months_freeze_thaw.csv

│   ├── AS_G8_3months_RT.csv

│   └── AS_G8_T0.csv

├── FREQUENCY_SWEEP

│   ├── FS_G1.csv

│   ├── FS_G2.csv

│   ├── FS_G3.csv

│   ├── FS_G4.csv

│   ├── FS_G5.csv

│   ├── FS_G6.csv

│   ├── FS_G7.csv

│   └── FS_G8.csv

├── pKa

│   ├── pKA_SCA.xlsx

│   └── pKa_SCG.xlsx

├── TEMPERATURE_SWEEP

│   ├── Temperature_Sweep_G1.csv

│   └── Temperature_Sweep_G2.csv

└── VISCOSITY

├── CSR_G1.csv

├── CSR_G2.csv

├── CSR_G3.csv

├── CSR_G4.csv

├── CSR_G5.csv

├── CSR_G6.csv

├── CSR_G7.csv

├── CSR_G8_3months_45C.csv

├── CSR_G8_3months_freeze_thaw.csv

├── CSR_G8_3months_rt.csv

└── CSR_G8_T0.csv

Methodologies

The rheological analyses were performed using an Anton Paar (Graz, Austria) MCR 92 rheometer. Rotational control shear rate analyses were performed at 23 °C collecting 37 data points at shear rate (%) between 0.001 and 1000 to evaluate the viscosity profile using a cone (d = 50 mm)/plane measuring system was used, with a gap of 0.098 mm. Oscillatory amplitude sweep experiments were performed at 25 °C using a Peltier control system and plate/plate geometry (shaft PP25/P2). Data points were collected (γ: 0.01–100%) using a constant angular frequency of 1 Hz. Temperature Sweeps were performed to predict products stability toward temperature cycles. The tests were carried out using the shaft PP25/P2 and were performed between 23 and 55 °C collecting 64 data points, one every 0.51 min. During the analysis, the frequency of 1 Hz was kept constant as well as the shear strain that was selected, from time to time, in the linear viscoelastic range of the sample. The analysis was then repeated on the same sample from 55 to 23 °C.

Detailed procedures for the preparation of each formulation were reported in the manuscript this dataset refers to (see “References” section).

Methodology for the determination of the apparent pKa.	
A XS pH70 Vio Portable pHmeter (XS Instruments, Carpi (MO), Italy) with a 2-pore steel T electrode was em-ployed for all pH measurements. The stated accuracy of the pH measurements is ± 0.1. The pH meter was calibrated before each experiment to check the response of the elec-trode. Depending on the desired concentration, considering a total volume of 2.5 mL for each sample, the required amount of gelator was suspended in Milli-Q® H2O and the pH was increased to 10.2 by adding NaOH 1 M. The samples were stirred to fully dissolve the gelator. The pKa values of gelator solutions were determined by titration via the addition of aliquots of a 1.0 M HCl (VWR Chemical, Milan, Italy) solution in triplicate. pH values were recorded until they reached a stable value after each addition during the titration process. Due to the strong and constant agitation applied, samples were always liquid during the titration experiments.

References
S. Chinelli, R. Stile, D. Giuri, C. Tomasini,  From Fundamental Self-Assembly Studies to Applications in Everyday Life: the Formation of a Supramolecular Shampoo, Gels 2026, https://doi.org/10.3390/gels12070589

FUNDINGS:

Sofia Chinelli thanks the Doctoral Scholarship financed by European Union—Next Generation EU (PNRR) funding (CUP J33C22001380009) pursuant to Ministerial Decree no. 352/2022, Mission 4, component 2 “From Research to Business”—Investment 3.3 “Introduction of innovative doctorates that meet the innovation needs of companies and promote the recruitment of researchers from companies”.

Roberta Stile thanks Doctoral Scholarship financed by European Union—Next Generation EU (PNRR) funding (CUP J33C24001450009) pursuant to Ministerial Decree no. 630/2024, Mission 4, component 2 “From Research to Business”—Investment 3.3 “Introduction of innovative doctorates that meet the in-novation needs of companies and promote the recruitment of researchers from companies".